## Slide 1: Scanning Tunneling Microscopy
Gregorio Jaca
October 9, 2025

## Slide 2
“I couldn’t stop looking at the images, it was entering a new world” Gerd Binnig

## Slide 3: Table of Contents
- Introduction and Motivation
Theoretical Minimum
  Principle of operation
  Measurement
Study of Highly Oriented Pyrolytic Graphite (HOPG)
  Atomic Steps
  Atomic Resolution
  Moiré effect
Conclusions and Discussion

## Slide 4: STM imaging
Scanning electron micrograph of the tardigrade Macrobiotus furciger with inset showing details of claw structure (Photography by S. McInnes)
IBM Corporation

## Slide 5: Tunneling
Trixler, Frank. (2013). Quantum Tunnelling to the Origin and Evolution of Life. Current organic chemistry. 17.

## Slide 6
Electrodes A and B are far apart.
Fermi level: A > B
The electrodes are brought into sub-nm proximity,
The Fermi levels are equalized
A contact potential is formed.
A bias Ut is applied.
The tunneling current flows
(filled states A) -> (empty states B)

## Slide 7: Study of Highly Oriented Pyrolytic Graphite (HOPG)

## Slide 8: Atomic Steps
Step height of around 3.3 ± 0.1 A
The interlayer spacing for graphite is approximately 34 A
Image of the graphite surface showing terraces
Altitude profiles at several terrace boundaries

## Slide 9: Atomic Resolution
Image an area with NO atomic terraces
Reduce surface-tip distance
Increase current set-point
Decrease bias voltage
Use 2D FFT filtering (noise reduction)
Triangular (not Hexagonal) patter emerges
The periodicity corresponds to the lattice constant.
Measured value: 2.5 ± 0.1 A
Theoretical value: 2.46 A
Plot with the peaks corresponding to the positions of the imaged carbon atoms.

## Slide 10: Moiré effect

## Slide 11: Moiré effect
Image two slightly rotated periodic gratings
Measured period of Moiré pattern:
D = 128.9 ± 1 A
Twist angle = 1.09 ± 0.03 °

## Slide 12: Conclusions and Discussion
- We measured Atomic Steps in Highly Oriented Pyrolytic Graphite
We measured the lattice constant of the sample with atomic resolution
We observed the Moiré pattern, measured its period and the rotation angle
We employed data cleaning and noise reduction techniques to ensure accuracy and precision in our measurements

## Slide 13: Thank you for the attention!
Please ask any questions you had during the presentation

## Slide 14: STM measurement device